SECTION 05521

HANDRAILS, RAILINGS, AND GUARDPOSTS

PART 1 - 	GENERAL

1-01	SCOPE:

A.	The Work of this Section shall consist of furnishing all labor, material, and equipment necessary for the installation of handrails, railings, and guard posts as shown on the Drawings and specified herein.

1-02	SUBMITTALS:

A.	Submit shop drawings, signed and sealed by a professional Engineer registered and active in the state of Louisiana, for all handrails and railings showing materials, configurations, dimensions, accessories, anchorage, etc.

PART 2 - 	PRODUCTS

2-01	MATERIALS:

A.	Comply with the requirements of the indicated specification.

1.	Steel Plates, Shapes and Bars (except plates to be cold-formed):  ASTM A36 and A992.

2.	Cold-Formed Steel Plates:  ASTM A283, Grade C.

3.	Steel Tubing:  ASTM A501, hot-formed, welded or seamless.

4.	Cold-Finished Steel Bars:  ASTM A108, grade as selected by fabricator.

5.	Cold-Drawn Steel Tubing:  ASTM A512; sunk drawn, butt-welded, cold-finished and stress relieved.

6.	Steel Pipe:  ASTM A53. Type E or Type S, Grade A; black finish unless galvanizing is indicated; standard weight (Schedule 40); unless otherwise shown or specified.

a.	Steel Finish: Shop prime paint, except where galvanized finish indicated.

7.	Malleable Iron Castings:  ASTM A47, grade as required.

8.	Nonshrink, Nonferrous Grout:  CE CRD C588.

9.	Woven Wire Mesh:  #10 wires, 1-1/2-inch diamond mesh, galvanized steel - ASTM A584-82 or ASTM A116-81.

10.	Guard posts Steel Pipe:  Comply with ASTM A120-84 pipe, steel, black and hot-dipped zinc coated (galvanized) welded and seamless for ordinary uses.

2-02	FABRICATION:

A.	General:  Form exposed work true to line and level with accurate angles and surfaces and straight sharp edges.  Ease exposed edges to a radius of approximately 1/32-inch, unless otherwise shown.

1. 	Form bent-metal corners to the smallest radius possible without causing grain separation or otherwise impairing the work.

B.	Non-welded Connections:  When acceptable to the Engineer, intermediate post-to-rail connections may be made using internal pipe sleeve locks and Allen screw fasteners.  Locking devices that do not produce flush, smooth, rigid, hairline joints will not be acceptable.  Weld other connections.

C.	Welded Connections:  Cope intersections of rails and posts, weld joints and grind smooth.  Butt weld end-to-end joints of railings or use welding connectors, at fabricator's option.

1.	At connections to steel supports, weld post directly to steel supports, unless otherwise indicated.

2.	Other methods of welding may be used when acceptable to Engineer.

3.	Weld corners and seams continuously and in accordance with the recommendations of AWS.  Grind exposed welds smooth and flush, to match and blend with adjoining surfaces.  Discoloration of finished surfaces will not be acceptable.

4.	Form exposed connections with flush, smooth, hairline joints, using concealed fasteners wherever possible.  Use exposed fasteners of the type shown, or if not shown, use Phillips Flathead (countersunk) screws or bolts.

5.	Provide for anchorage of the type shown, coordinated with the supporting structure.  Fabricate and space anchoring devices as shown and as required to provide adequate support.

D.	Brackets, Flanges, and Anchors:  Provide brackets, flanges, and anchors for railing posts and for handrail supports.  Furnish inserts and sleeves as required for anchorage to concrete or masonry work.

1.	Furnish cast metal brackets, flanges, and exposed anchors of the same material and finish as supported rails, unless otherwise indicated.

2. 	Galvanize all steel railings, including pipe, fittings, brackets, fasteners and other ferrous metal components after cutting, drilling and fabrication.

PART 3 - 	EXECUTION

3-01	INSTALLATION:

A. 	Fastening to In-Place Construction:  Provide anchorage devices and fasteners where necessary for securing handrails and railing items to in-place construction; including, threaded fasteners for concrete and masonry inserts, toggle bolts, through bolts, lag bolts and other connectors as required.  Use railing manufacturer's standard method of installation when acceptable to Engineer.

B. 	Cutting, Fitting and Placement:  Perform cutting, drilling and fitting required for installation.  Set the work accurately in location, alignment and elevation, plumb, level, true and free of rack, measured from established lines and levels.  Fit exposed connections accurately together to form tight hairline joints.  Weld connections that are not to be left as exposed joints but cannot be shop-welded because of shipping size limitations.  Grind joints smooth and touch up with heavy zinc rich coating product. Do not weld, cut or abrade the surfaces of units that have been coated or finished after fabrication, and are intended for field connections.  Adjust railings prior to securing in place to ensure proper matching at butting joints and correct alignment throughout their length.  Space posts not more than 5 feet on centers, unless otherwise shown.  Plumb posts in each direction.  Secure posts and rail ends to building construction as follows:

1. 	Anchor posts in concrete by means of pipe sleeves set and anchored into the concrete.  Provide sleeves of galvanized, steel pipe, not less than 6 inches long and having an inside diameter not less than 1/2-inch greater than the outside diameter of the inserted pipe post.  Provide steel plate closure secured to the bottom of the sleeve and of width and length not less than 1-inch greater than the outside diameter of the sleeve.  After the posts have been inserted into the sleeves, fill the annular space between post and sleeve solid with nonshrink, nonferrous grout.  Cover anchorage joint with a round metal flange to match post.

C. 	Secure handrails to walls with wall brackets and end fittings.  Provide brackets with not less than 1-1/2-inch clearance from inside face to handrail to the finish wall surface.  Drill wall plate portion of the bracket to receive one bolt, unless otherwise indicated for concealed anchorage.  Locate brackets as indicated or, if not indicated, at not more than 8-feet-0-inch off-center.  Provide flush-type wall return fittings with the same projection as that specified for wall brackets.  Secure wall brackets and wall return fittings to building construction as follows:

1. 	For concrete and solid masonry anchorage, use bolt anchor expansion shields and lag bolts.

2. 	For hollow masonry anchorage, use toggle bolts having square heads.

3. 	For drywall anchorage, provide horizontal wood blocking connecting consecutive studs, use toggle bolts having square heads.

D. 	Guardposts:  Erect guardposts plumb and aligned and located as shown on contract drawings, footings as shown on structural drawings.  Fill 8-inch diameter steel pipes with 3000 psi concrete and finish top smooth and convex.  Weld guardposts in mitered joints and grind smooth and flush.  Paint and finish as required by the Engineer.  Unless otherwise indicated, paint as specified for structural work in SECTION 05100.

E. Wire Mesh:  Fixed wire mesh fabric with tension bars at all four sides and connecting plates welded to the railing and posts.  Stretch fabric between tension bars as required.  Install tension bars centered and equally spaced parallel to posts and rail pipes.  Comply with AWS Code for procedures, appearance, and quality of welds, and for methods used in correcting welding work.

***END OF SECTION***